## Slide 1: QualiFibre Qualification and Diagnosis of Carbon and Glass Fibre-Reinforced Composites with Non-Destructive Measurement Technologies
Workpackage 2
28/01/2015, Halle, Germany

## Slide 2
Workpackage 2
Title: Testing, quality parameters and defects acquisition
Objectives:
Relevant defect parameters are identified
Reliable methods to insert defined defect structures into glass- and carbon-fibre materials have been implemented
Test samples have been designed and produced
Testing methods to recognize artificial defect structures have been established
Qualification method has been developed to classify defects properly and reliable
Concept of experimental set-up for multi sensor analysis has been developed

## Slide 3: Task 2.1
Title: Definition of defect analysis, material parameter acquisition and qualification
Task Leader: EMPA
Goals:
  Analysis of different kinds of defects
  Categorisation of defects
  Qualification of defects
Notes: ... that means:
1) WHAT are the relevant defects in selected industries / branches / products?
2) HOW can we detect them in a ...
- cheap,
- fast and
- reliable way?

## Slide 4: Task 2.1
Analysis of different kinds of defects (examples) ... using ultrasonic

## Slide 5: Task 2.1
Analysis of different kinds of defects (examples) ... using thermography

## Slide 6: Task 2.1
Analysis of different kinds of defects (examples) ... using CT

## Slide 7: Task 2.1
Analysis of different kinds of defects (examples) ... using dark field

## Slide 8: Task 2.1
Defect Structure Qualification and Characterization Method Matrix

## Slide 9: Task 2.1: Did we reach our goals?
Goals:
  Analysis of different kinds of defects
  Categorisation of defects
  Qualification of defects



Notes: ... that means:
1) WHAT are the relevant defects in selected industries / branches / products?
2) HOW can we detect them in a ...
- cheap,
- fast and
- reliable way?

## Slide 10: Task 2.2
Title: Development of adequate test parts and samples with defined defects. Elaboration of a test plan for specified parameter/data resampling
Task Leader: STW
Goals:
  Development of test-part mould for production
  Reproducible production of test-parts with defined defects
  Elaboration of a test-plan for multi-sensor-data acquisition
Notes: ... that means:
1) WHAT are the relevant defects in selected industries / branches / products?
2) HOW can we detect them in a ...
- cheap,
- fast and
- reliable way?

## Slide 11: Task 2.2
The Mould for the test parts
Mould for test part manufacturing
I

## Slide 12: Task 2.2
The Mould for the test parts
Cross section of the mould for flat and 3D-test parts

## Slide 13: Task 2.2
The production of the Test parts

## Slide 14: Task 2.2
The production of the Test parts – post-processing

## Slide 15: Task 2.2
Test parts with defined defects

## Slide 16: Task 2.2
Test parts – pre damaging

## Slide 17: Task 2.2
Test plan
testparts with defined defects
different sensors of one kind (US or TG or CT ...)
tests regarding visibility, detectability, resolution, scan-time etc.

## Slide 18: Task 2.2: Did we reach our goals?
Goals:
  Development of test-part mould for production
  Reproducible production of test-parts with defined defects
  Elaboration of a test-plan for multi-sensor-data acquisition




## Slide 19: Task 2.3
Title: Development of the test plan for sensor type selection considering the different parameter/defect types and specification of the used sensors
Task Leader: STW
Goals:
  design of a methodology of multi-sensor measurement equipment
  development of a test plan, covering all relevant defect structures

## Slide 20: Task 2.3
End users test parts
trunk part from Daimler AG

## Slide 21: Task 2.3
Test plan
End users test parts
Prove of concept tests
Performance tests to locate the optimization potential

## Slide 22: Task 2.3: Did we reach our goals?
Goals:
  design of a methodology of multi-sensor measurement equipment
  development of a test plan, covering all relevant defect structures


Notes: ... that means:
1) WHAT are the relevant defects in selected industries / branches / products?
2) HOW can we detect them in a ...
- cheap,
- fast and
- reliable way?

## Slide 23: Task 2.4
Title: On board overload sensing
Task Leader: STW
Goals:
  analysis of possible technical solutions with regard of possible usability in field monitoring and status documentation of CRP/GRP objects

## Slide 24: Task 2.4
Strain gauges
Quelle: http://upload.wikimedia.org/wikipedia/commons/thumb/c/c3/StrainGaugeVisualization.svg/400px-StrainGaugeVisualization.svg.png
Quelle: Fraunhofer IZM (idw) http://www.extremnews.com/berichte/wissenschaft/2ea51411dfa71ee/d2ed1411dfa7221/

## Slide 25: Task 2.4
Powersense and structure-borne-noise-/impact-noise-analysis
Quelle: SEFAR PowerSense, Quelle: Sefar AG, CH http://www.sefar.com/data/docs/en/7281/SF-Smart-Fabrics-PowerSens-07.jpg?variant=44253
Quelle:
ATZ - Automobiltechnische Zeitschrift Ausgabe 02/2008 Seite 160-165, Autor(en): Dipl.-Ing. (FH) Marinus Luegmair, Dipl.-Ing. (FH) Lucas Oestreicher

## Slide 26: Task 2.4: Did we reach our goals?
Goals:
  analysis of possible technical solutions with regard of possible usability in field monitoring and status documentation of CRP/GRP objects
  BUT: further investigation an d research necessary!
  Especially: Production of test parts.
  And also: Systematic analysis of usability during complete lifetime of a product.
  To be continued!

Notes: ... that means:
1) WHAT are the relevant defects in selected industries / branches / products?
2) HOW can we detect them in a ...
- cheap,
- fast and
- reliable way?

## Slide 27: Task 2.5
Title: Conceptual development of experimental set-up for all sensors and application requirements
Task Leader: STW
Goals:
  conceptual definition of multi-sensor equipment

## Slide 28: Task 2.5
Conceptual hardware set-up dark field / CT at EMPA

## Slide 29: Task 2.5
Conceptual hardware set-up thermography at Winterthur Instruments

## Slide 30: Task 2.5
Conceptual hardware set-up CT at Rayscan

## Slide 31: Task 2.5
Conceptual hardware set-up ultrasonic at Sonotec

## Slide 32: Task 2.5
Conceptual software set-up
 Details will be presented in WP3

## Slide 33: WP 2: Conclusion
Did we reach the objectives of our Workpackage?
Relevant defect parameters are identified
Reliable methods to insert defined defect structures into glass- and carbon-fibre materials have been implemented
Test samples have been designed and produced
Testing methods to recognize artificial defect structures have been established
Qualification method has been developed to classify defects properly and reliable
Concept of experimental set-up for multi sensor analysis has been developed





